Keszler, Bram 23.05.2024

Maccari, 10.06.2024

Revision of manuscript PMG-24-0005 – Answer to the reviewer comments

Field assisted sintering and spark plasma texturing of Nd-Fe-B magnets with tailored anisotropic magnetic properties

Reviewer #1:

In the following manuscript, SPS sintering/hot deformation and flash hot deformation has been presented. The manuscript lacks adequate story-telling and is written in a manner that is complex to read from the perspective of numerous SPS parameters that have been randomly intermixed. The presentation of magnetic properties with respect to microstructure is incomplete as there is hardly any discussion on the results, and self-citations is plainly obvious in this work. Either this report should be fragmented to separate SPS hot deformation from Flash hot deformation, or it must be reformulated in a manner that follows a structure and is lucid for readers to grasp critical information.

This manuscript must be rewritten and resubmitted and should not be accepted in present state.

We thank the reviewer for carefully reading and commenting our manuscript even if the original submission does not fulfil the standards of “Powder Metallurgy”. We completely revised the manuscript according to the manifold recommendations and submit it as new manuscript. In the new submission, we focus on doing hot compaction and hot deformation of melt-spun Nd-Fe-B powders (MQU-F) by FAST/SPS. For clarity of the manuscript, we completely removed all results on Flash SPS, which were already published earlier. For hot deformation of melt-spun Nd-Fe-B powders by FAST/SPS, we compared two routes. In the first approach, we started the hot deformation process from a at low temperature (500°C) pre-sintered, still porous semi-finished part, which is attractive due to remaining the primary grain size of the melt-spun powder until applying the hot deformation step. Under this condition, the risk of anomalous grain growth during hot deformation should become reduced. This approach is also attractive for direct reprocessing of scrap from end-of life (EOL) magnets due to reducing further grain growth during this secondary hot-deformation step. The potential of this approach has been already shown when using Flash SPS for hot deformation. In the second approach, we adapt the standard processing of hot deformed magnets to a two-step FAST/SPS process, starting with the production of a dense, semi-finished part by FAST/SPS at a temperature above the melting point of the grain boundary phase. Here, parameters were optimized to reduce grain growth in the semi-finished part to a minimum. Then, hot deformation parameters were optimized to achieve a good balance between coercivity and remanence. The second approach deals with showing the potential and remaining challenges of doing the hot deformation step by FAST/SPS. An interesting – not completely understood result – is the fact that FAST/SPS requires higher deformation degrees than conventionally hot deformed magnets to achieve comparable magnetic properties. On a midterm scale, we plan to apply FAST/SPS as alternative hot deformation technology for the processing of high performing magnets starting from Nd-Fe-B powders made by direct melt-spinning of EOL magnets.

Bold Black indicates correction/comments and Bold Red scheme marks down the questions which need to be addressed.

1) Abstract/Page 3: The abstract is very general and hardly provides any technical details and does not lay enough emphasis on which method is better FAST or Flash, besides description of precursor type is also missing. There is a big difference in FAST and Flash methods for microcrystalline powder, HDDR and melt spun ribbons. So, the abstract should be written with some technical details without going too much in to details and share how hypothesis developed towards potential aims of the study. The last five lines are a summary, so these are not required in an abstract. It needs complete revision.

Answer: Thank you for your comment. Abstract has been edited. Now, it introduces the two approaches mentioned before for applying FAST/SPS as alternative technology for hot deformation of Nd-Fe-B magnets. Starting powder has also been mentioned to be specifically nanocrystalline melt-spun powder. The abstract concludes with a benchmark to conventionally hot deformed Nd-Fe-B magnets.

2) Introduction/Page 5: The melt spun ribbons are isotropic, whereas the HDDR powder is anisotropic. The authors do not make an elaboration on the HDDR route as an alternative to melt spun ribbons and cite the potential benefits of the latter over former system to provide an argument as to why nanocrystalline ribbons were selected in this study.

Answer: An explanation as to why we prefer isotropic melt-spun powder over anisotropic HDDR powder is given now in the introduction.

3) Introduction/Page 5: From where the authors have taken the images in Figure 1? Please provide citation in case these figures are adopted.

Answer: In the revised manuscript, we almost completely skipped refering to textbook knowledge including omitting the former Figures 1 and 2. The focus of the revised manuscript is now an experimental study to investigate the potential of FAST/SPS as alternative technology for the hot deformation of Nd-Fe-B magnets.

4) Introduction/Page 6: ‘Nevertheless, there is no consensus in the literature on the reason behind the texture development.’ The authors certainly have not researched the literature enough on this scope, so I request revisiting previous literature on hot deformation of Nd-Fe-B melt-spun ribbons. Please provide more details on what recent review from Hioki et al. [5] infers related to texture development and explain Figure 2 appropriately. It would be better if the authors can formulate a similar figure on their own. An important criterion here  is to observe how Nd-rich phase migrates and reformulate, in turn shaping textured grains from hot pressing to hot forging/deformation stage. Elaborate this figure.

Answer: Thank you for this important comment. We tried to shortly summarize the main mechanisms of microstructure formation during hot deformation as discussed by Hioki et al. Since we did not conduct a detailed study on anisotropic grain growth and influence of the temporarily molten Nd-rich grain boundary phase during hot deformation by FAST/SPS, we feel not able to seriously adapt the figure of Hioki et al. to the specific conditions of FAST/SPS. Therefore, we skipped former Figure 2 and just summarized the hot deformation mechanisms from the literature in compact form.

5) Introduction/Page 6: When the authors talk about electroplastic effects, which phase predominantly undergoes plastic deformation and how the hard phase deforms under flow stress effects should be elaborated. So far, everything the Introduction has provided are trivial sentences detailing the process, whereas the mechanism related to principal phenomena is missing, be it texture development or electroplastic flow in SPS.

Answer: At current state, we do not have a sound experimental confirmation that electroplasticity plays a significant role during hot deformation via FAST/SPS. Therefore, we decided to completely remove our speculation that it might play a role. Nevertheless, we have planned to conduct specific experimental series with/without current flow through the sample to clarify this possible effect. In the present work, it is of greater interest to us to demonstrate that ECAS is capable of generating magnets with fine-tuned microstructure through the manipulation of the parameters.

6) Introduction/Page 7: Use single acronym for SPS processes, and later for FAST and Flash. Do not introduce ECAS too many times to replace SPS/FAST. Later it is important to highlight SPS processes adapted for Nd-Fe-B system only and provide details of most critical data from each literature.

Answer: The acronym FAST/SPS (= Field assisted sintering technology/spark plasma sintering) is generally used for describing the technology used in this work. With respect to the literature [Noudem 2012], spark plasma texturing (SPT) is introduced as new acronym for the hot deformation step in a FAST/SPS device, which also helps to avoid possible misunderstanding of each step is being discussed in our work.

7) Introduction/Page 8: ‘Unfortunately, information about exact tool design, complete set of deformation parameters, dimensional accuracy and microstructural homogeneity is rare [21,22,23,24,26,27,30]’. This is a vague statement and authors must reflect on literature data properly. Almost every article should provide details on processing temperatures, pressure and the die geometries, while microstructural homogeneity may vary but the texture formation in hot forged melt-spun ribbons should appear very similar. The authors have added citations of several papers for a single statement.

How can a single statement reflect so much published data, and this should invalidate the current hypothesis. Explain the cited literature properly rather simply filling in self-citations or similar.

Answer: The statement has been edited according to your recommendation and each cited paper was examined for information that is missing that could be vital to reproducibility and mentioned. Furthermore, we added citations of the recent works of Ikram et al., who described texturing of recycled HDDR magnets by spark plasma sintering in detail [Ikram 2019, Ikram 2020].

8) Materials and Methods/Page 8: How is the present study different than the work done by E. Castle et al. [15]? The goals of the present study should encompass the shortcomings of previous work(s) and build upon that. This report does not specify what was inadequate or inappropriate from existing research and experimental design that the authors had pursued. How the setup is different and how characterization can be different needs to be highlighted in the final segment of Introduction.

Previous works have shown that at 50 MPa relative to 10 mm die can create > 95% densification, so how can you limit consolidation to less than 75% as a hypothesis should be explained as well. Then why would you do a 45 MPa at 725 OC instead of 50 MPa, and why not 30 or 40 MPa instead? How die size influences electoplastic deformation in FAST state? Explain the reason behind the selection of parameters for FAST and Flash processes.

Answer: The focus of the revised manuscript has been changed into more of a baseline study for conducting hot deformation of Nd-Fe-B magnets by FAST/SPS, referred to as SPT in the paper. For clarity, the part on hot deformation via Flash SPS has been skipped. We tried to explain more clearly the choice of our FAST/SPS parameter sets.

9) Materials and Methods/Page 10: How was 46% tapping density measured? How was the theoretical density calculated as well?

Answer: Theoretical density is considered full density of Nd-Fe-B (7.55 g/cm3). Tap density changed in this paragraph to Fraunhofer's measurement for consistency.

10) Materials and Methods/Page 11: Why the dwell time at 500 °C was not increased during presintering stage to several minutes and why only 30 s, when it would be clear that a ~50% tapping density would eventually lead to marginally adequate 75% densification at these temperature-pressure conditions? Why not 600 – 650 °C with 50 MPa pressure and you could already reach >95% densification, and why it was considered appropriate to go above ternary transition temperature in order to sinter the pellet similar to hot pressing. So, at 700 OC, this is not pre-sintering anymore. Obviously, there are other pressure compaction strategies to increase the densification at lower temperatures, but authors opted to go above ternary transition temperature and they still rckon it as pre-sintering is a false statement. You need to understand both your SPS machine and Nd-Fe phase diagram.

Answer: The pre-sintering at 500 °C was only utilized to generate pellets designed to withstand the minimum load required for operation of the FAST/SPS device, which is prerequisite for doing hot deformation in this device. At the time of these experiments, development of the microstructure was relegated primarily to the deformation stage, and the pre-sintering stage was utilized for mechanical stability. Samples compacted above 700 °C will no longer be listed as pre-sintered, instead as hot-compacted.

11) Materials and Methods/Page 12: I am actually very surprised to see abnormal grain growth at just 750 °C, while the pressure is only 50 MPa. This is a dubious claim without paying attention to grain growth kinetics and leveraging proof of it from microstructure standpoint. How has abnormal grain growth occurred? Please explain from phase transition and thermal kinetics standpoint, not just simply stating a fact what you see. The details in Figure 5, I would say are rather relative than simply calling them as abnormal grain growth. Better to add higher resolution and higher magnification details to justify these claims. What I do see in Figure 5 (b) is a facet ~10 micron in size along the cross-section that has different growth direction. Why this may have occurred would be interesting to read from your standpoint, but it is very much to do with SPS pressure and Nd-rich phase rotation and sliding along the particle boundary.

Typically, the abnormal grain growth begins after the onset of 820 °C in Nd-Fe-B nanocrystalline systems (melt-spun and HDDR), and then authors were changing parameters here and there like trial and error without reviewing previous literature on hot deformation works with SPS.

Answer: Likely grain growth is happening due to Joule heating. A similar effect was seen in Keszler et al. and Mishra et al. due to the influence of the electrical field. This could lead to localized hot-spots at contact points, leading to grain growth at particle edges. (Fraunhofer IWKS - can you add a larger or higher mag image for Figure 5?)

12) Materials and Methods/Page 12: There is no need to mention at Forschungszentrum Jülich/Fraunhofer IWKS we had this and there we had this. Simply write about methodology that in this present study…

Answer: Noted and edited. For clarity, Forschungszentrum Jülich and Fraunhofer IWKS are just mentioned in the introduction now. We believe that this is also important, since different devices were used and tools, which also gives basis about the reproducibility of the study.

13) Materials and Methods/Page 12: ‘formation of the transient liquid phase is avoided reliably.’ You do not understand the phase diagram as this is a false statement. The ternary transition

temperature is way lower than 725 OC, so you already breached that when sintering (there is no presintering stage either).

Answer: Thank you for this important hint. The formation of the liquid grain boundary phase when hot-compaction is done at 725°C is mentioned now.

14) Materials and Methods/Page 12: ‘After achieving the aspired deformation temperature, the deformation load was varied between 50 and 500 MPa followed by a short dwell time of 10 s.’

How were these parameters selected and why for hot deformation 50 MPa only, which translates to quite less load in kN for the die size 30 mm?

Answer: Full deformation of the sample up to the die wall of the FAST/SPS tool was observed with a 32 MPa load. Therefore, 50 MPa was chosen as a baseline as it doesn't differ too far from 32 MPa and can be easily compared with pressures 5-10 times higher.

15) Materials and Methods/Page 12: ‘For conducting this kind of experiments, Φ 20 mm samples pre-sintered at 500°C were placed in a Φ 30 mm FAST/SPS tool, which was lined with a 0.38 mm thick graphite foil (SGL Carbon, SIGRAFEX).’

Now again 500 °C is back when you had earlier discarded these conditions in favor of sintering (presintering) above ternary transition temperature? The methodology part needs serious revision as authors pick up some details and then in next paragraph start something else which is contradicting to overall methodology.

Answer: We agree that the description of experiments in the original submission is confuse. In the revised manuscript, for sintering porous, semi-finished samples 500 °C was selected to avoid grain growth before applying SPT. Hopefully, the more distinct separation of the two approaches makes it more clear in the revised manuscript.

16) Materials and Methods/Page 13: ‘Then the sample was heated with a defined heating rate to the aspired deformation temperature.’ Mention the heating rate and deformation temperature-pressure conditions for each respective experiment.

Answer: Noted and done

17) Materials and Methods/Page 13: ‘In the P-series, the pressure was varied to 100, 200 and 500 MPa at a constant temperature of 800°C. For the current pulse ratio (CPR), we used the standard configuration of our FAST/SPS 12:2.’

You explained before that for 50 MPa, a temperature of 750 OC lead to so-called abnormal grain growth. And now at 500 MPa, you are doing hot deformation. Why? What defines your hypothesis? This is absolutely ridiculous to read that there is simply no sense out of experimental methodology, just randomly picking up parameters. And previously you stated 2:2 current pulse ratio better suited to your design, why are you back to 12:2 now? You did not explain for readers what is 12 and what is 2 (with units) in this CPR.

Answer: The grain growth at 750 °C during pre-compaction was not excessive. The reason for the choice of temperatures was based on what was observed in our Flash SPS experiments. When the 'flash' phase occurred (35 kW in 30 sec), the sample often reached temperatures around 800 C. We were able to achieve decent magnetic performance from these experiments [Mishra 2023]. Therefore, we translated the maximum temperature from the flash SPS experiments to our SPT experiments.

Since we did not change the current pulse ratio in our experiments, this information was omitted in the revised manuscript.

18) Materials and Methods/Page 14: ‘At Fraunhofer IWKS, the deformation experiments deal with the conventional hot deformation of anisotropic Nd-Fe-B magnets, but using FAST/SPS technique for the hot deformation step.’

Try read this statement from a third person perspective and you will see how confusing it is. When you try to enforce distinguishing experimental work at two different places in parallel, it becomes a total mess to identify what authors are presenting, and then you are moving between the parameters without clarity. Why is temperature set here at 750 °C instead of 800 °C now? You should only use either kN or MPa for SPS pressures, not both.

How it reads as a difference between Fraunhofer IWKS and Forschungszentrum Jülich is different die sizes for sintering and hot deformation. It is very fuzzy and ambiguous to read and understand what exactly is happening at multiple places and multiple different strategies to sinter/pre-sinter and hot deformation.

Answer: This has hopefully been rectified by clear separation of the SPT sections (semi-dense vs. dense) and indication that these experiments were occurring parallel to each other. Therefore, not all strategies are shared.

19) Materials and Methods/Page 16: For a more detailed description, see the recent work of Maccari et al. [32]. If I have to read the work of Maccari et al. [32] then why is there a need for this research?

Answer: Section on Flash SPS has been deleted.

20) Materials and Methods/Page 16: Figure 7b demonstrates the potential of Flash SPS for net shaping of Nd-Fe-B magnets, but the sample was not characterized regarding their magnetic properties so far. Related results will be published in a separate manuscript soon.

I think it is pivotal to add magnetic properties in the same manuscript, else this one can be rejected entirely.

Answer: Section on Flash SPS has been deleted.

21) Materials and Methods/Page 17: Why is relative density less than 100% in case of Flash hot

deformation even though greater than 70% height reduction has been achieved?

Answer: Section of Flash SPS has been deleted. In the case of Flash SPS, samples were hot deformed without an outer die leading to frayed edges with some undefined residual porosity.

22) Results/Page 20: Why the magnetic properties especially HCi of P800-100 are higher than P800-50 and P750-50, but then again Br is higher than other two as well?

What is special in processing of HDS701 and HDS704 samples that both their coercivity and remanence are higher than other samples? The Br values for HDS samples are considerably higher at 70 MPa than 500 MPa deformed samples, why? My concern with results section is that the authors only comment on results or present in form of a table but there is hardly any explanation on how the parameters prompted towards the magnetic properties and microstructure. The variation in parameters and then citing them in results section is mostly in inappropriate manner which does not follow a pattern, and this randomization of results presentation makes understanding of overall script quite cumbersome.

The deformation curve is very relative to how particles of certain size are present within the SPS dies. If there is a bigger variation in particle size, we can anticipate a bigger deformation curve as gap filling occurs which can also lead to bigger misalignment of particles under pressure in SPS, and vice versa.

Why additional pressure hold during the cooling phase was not established, as it could have resulted in approaching nearly full densification in Flash SPS samples?

Answer: Thank you for your comment. It has been attempted to make it clearer that these experimental series were occurring in parallel to each other without collaboration at the time. Many of the same observations were noted to be seen, e.g., grain growth at pressures above 100 MPa + 800 C, misalignment of grains when the starting compact was not fully dense. The authors hope there is a clearer thread among the discussion section after this revision.

23) Results/Page 24: Now in Figure 10 (a) which is BSE SEM image of surface and not cross-section, under 100 MPa deformation there are well-defined particle boundaries perpendicular to the direction of direction of pressing, whereas in Figure 10 (b), te particle boundaries are rather random. Some follow direction of pressing while some are perpendicular to it.

What happens to the particle boundary Nd-rich phase and how do you anticipate intergranular Nd-rich phase to flow under the application of higher deformation pressures as the grains come under c-axis alignment? What is the origin of larger sized grains and their texture under higher deformation pressures at the particle boundaries richer with Nd-intergranular phase? There is simply no discussion of results whatso ever present.

Answer: This figure is a cross section. Yes, the particle boundaries are random and likely due to how the powder is compacted during the process. Some particle boundaries are perpendicular as the boundaries of the particles do not simply dissolve into the matrix and maintain their form even during deformation. This could be due to oxides on the surfaces of the particles preventing full Nd grain boundary phase liquid formation.

24) Results/26: How the grain growth in Figure 12 has translated to magnetic properties variation, please write within results section?

Answer: Answer still missed

25) Results/Page 29: The magnification level of different trends in microstructure should be at the same level, for instance Figure 10 cannot be clearly related to Figure 14, and so on.

Answer: Figure 14 has been omitted in the revised manuscript.

26) Results/Line 254 – 256: I really do not see a benefit of pre-heating in Flash SPS stage towards c-axis texture considering this short dwell is well below the ternary transition temperature, so pre-heating at 251 °C is of course not of any benefit, while at 600 °C the authors can comment related to porosity control. At the end of this section and from Figure 15, what exactly authors want to infer is then contradicting to their conclusion that pre-heating has benefits towards texturing and grain growth. How this texture and grain growth relates to reduction in coercivity is plainly missing, so discuss thoroughly.

Answer: Section on Flash SPS has been deleted

27) Results/Page 30: ‘Densification without significant anisotropic grain growth and texture development is indicated if remanence stays near to 0.8.’

What is 0.8 here, is it Br = 0.8 T or Mr/MS = 0.8?

Answer: It is the Br value, this information has been updated accordingly.

28) Results/Page 32: ‘As result of hot deformation, the coercivity is reduced by ca. 20%, while the saturation magnetization is increased by ca. 32%.’

How can you increase the saturation magnetization without changing chemistry at atomic scale? This is description of remanent magnetization and not saturation which for Nd-Fe-B is 1.6 T.

Answer: The term “saturation magnetization” has been changed to “remanence”. Previously the term was incorrectly used, since it is an intrinsic magnetic property, as correctly mentioned by the reviewer.

29) Results/Page 34: Where did you see electroplasticity and how can you confirm this phenomenon occurred during the Flash SPS stage when there is no visible proof to it? Under Flash SPS, this can rather be simply be pressure induced deformation, as I did not see any indication of plastic flow under high change density in Flash SPS.

Answer: We agree that at current state of investigation, all discussion on possible occurrence of electroplasticity is just speculation. Therefore, we deleted the related sections. Experimental series with/without current flow through the sample are planned to focus on this aspect and to achieve more reliable conclusions on electroplasticity.

30) Results/Page 34: Self-citations is plainly very obvious in this study. This study is very inconclusive and has several technical mistakes highlighted above. It would need special and concertized efforts to reformulate this manuscript. I would suggest to split the work between SPS hot deformation and Flash SPS in to two manuscripts as there is severe lack of description of results and discussion. Or to reorganize in a manner that there is a proper flow in which reader does not get lost between so many different and yet similar SPS parameters. I strongly recommend to re-make this manuscript and submit again. Abstract and conclusion also need proper revision.

Answer: We agree that the original submission does not fulfil the standard of “Powder Metallurgy”. Therefore, we completely skipped the part about Flash SPS and focused the revised manuscript only on hot deformation via FAST/SPS, starting from porous and dense, semi-finished parts. In this sense, complete structure of the manuscript has been revised and we hope that our strategy and presentation of results becomes more clear now.

31) Considering Prof. Gutfleisch is part of the contributing authors, I strongly recommend to get this manuscript thoroughly proofread prior to submission as the quality of this report is inarguably very low and does not do justice to his portfolio. The author’s contributions in the manuscript should also be detailed. In the present state, I cannot vouch for even major revision of this manuscript, thus it should be rejected in favor of total reformulation.

Answer: Before submission of the revised and total reformed manuscript, we did carefully proofread. Due to substantial changes, we decided to submit the revised manuscript as new submission. Authors contributions are mentioned in the revised manuscript now. Again, we thank the reviewer taking so much effort to carefully review our original manuscript. Your recommendations helped a lot for restructuring our work.

Reviewer #2:

Keszler Monica et. al performed and demonstrated that preparing anisotropic Nd-Fe-B magnets via FAST/SPS and Flash SPS at different lab-scale devices at two labs, comparing the differences in microstructure and properties caused by various parameters (such as, temperature, pressure, heating rate and so on). This work reveals that Flash SPS has the potential to control Nd-Fe-B anisotropic grain growth and texture development. I think the work is conceptually interesting and could be appropriate for this journal. However, the following issues need to be resolved before the article is published:

1. Page 11 Line 3. The authors mention “The sample compacted at 725°C (Figure 5b) is fully dense with the melt spun flakes well aligned in whole sample volume and pronounced grain growth was not observed”. However, in Fig.5 b), obvious grain growth can be observed, and clearly pointed out in the graphic illustration. Please give an explaination.

Answer: Thank you for the comment. The document has been updated to mention that grain growth may happen at contact points between particles due to localized Joule heating.

2. Page 21 line 34. “In this experimental approach, the highest remanence value (1.25 T) was obtained…”. Here, the corresponding B-H curve should be provided to prove your opinion.

Answer: Thank you. The requested B-H curve was generated and is included as new Figure 6.

3. Page 23 line 26. How can it be shown that hot deformed grains at the lower temperature of 725 °C does not grow and maintained good orientation? Appropriate supporting materials should be provided.

Answer: XXX

4. Page 25 line 27. There is no evidence given that the deformation of stage (I) has begun when the preheating temperature is 300°C. It is hoped that the evidence will be given rather than a simple expression.

Answer: Section on Flash SPS has been deleted in the revised manuscript.

5. Page 27. line 40. This part, a verification of the hypothesis in Page 25, is interspersed between the two paragraphs with changes in macro- and microstructure and the reasons after Flash SPS. It is logically far-fetched to discuss the hypothesis and validation separately in this way.

Answer: Section on Flash SPS has been deleted in the revised manuscript.

6. In your tables you list the labeling of each process, but rather than using these labels in your presentation in the text you just state the process conditions? This makes your presentation not very clear!

Answer: This has been rectified. Sample names are now being used within the text and the figure captions.

7. The performance of the magnets at various parameters you have just listed in table4 in the form of numbers, would you please provide the corresponding B-H curves or references to prove it?

Answer: Yes, the requested B-H curves are provided now. Thank you for the suggestion.

Reviewer #3:

The researchers describe the densification of pre-compacted NdFeB by either spark plasma sintering or flash sintering. While in the latter case, densification is achieved by a high current pulse through the sample, for spark plasma sintering, a high mechanical load is applied after reaching deformation temperature, leading more to a sinter forging approach. A parameter study has been performed to identify the impact of deformation temperature and pressure in case of spark plasma sintering as well as pre-heating temperature in case of flash sintering on microstructure and magnetic properties.

Language and style should be improved but usually it is possible to understand the meaning of the sentences. SI units should be used exclusively.

Answer: Language was improved and SI units are exclusively used now.

The introduction is somewhat confusing and lengthy, and it is not clear if the paper is supposed to be a (quite unstructured) review or a research article (it finally becomes clearer on p8/line 25). Nd-Fe-B is alternatingly used with Nd2Fe14B; for nanocrystalline material there are flakes and without milling it becomes powders; then there are fibres/a fibre texture (p4/line 55). P5/line 44 suddenly introduces a new term (ECAS) instead of field assisted sintering technologies which is initially used. EDS is later described what makes the reader guess that this technology will also be used in the experiments. Also, details of the experimental plan are described in the introduction.

The section “Experimental” is also unstructured, lengthy and includes results and discussion. The authors should focus on what was actually done to prepare the samples. For the mechanical load, kN and MPa are both used. Why is the process chain shown for approach two only? How was the temperature measured?

Answer: We agree that the structure of the paper needed significant revision and the scope of the paper must become clearer. Therefore, the manuscript was completely restructured now focusing on experimental results and their discussion. We carefully checked to revised manuscript to avoid mixing of experimental part and results.

Results section introduces text book knowledge (“A high remanence means that…“) and contains a lot of discussion and statements („it becomes clear that these technologies have the potential to become competitive, but…). 3.1 and further starts with repeating the experimental section.

Answer: We carefully checked the manuscript to avoid general statements. We skipped all explanations just repeating textbook knowledge. Now, the focus of the manuscript is on experimental results and their discussion.

Some specific points:

P9/line 28: Why is the material pre-sintered in the SPS to withstand densification in the SPS?

Answer: Thank you for your comment. The powder is pre-sintered in this case for two reasons. In the case of the low-temperature, semi-dense compact, the powder is pre-sintered in order to create good electrical contact during the SPT process. For the dense compact, the powder is pre-compacted as a stand-in for the hot-compaction step of hot deformation.

P9/line 41: the foil is called Sigraflex

Answer: Thank you, the mistake has been amended.

P9/line 54: Why is there a transient liquid phase in pre-alloyed material?

Answer: In Nd-Fe-B, grains are kept isolated from one another through an Nd-rich boundary phase. This has a lower melting temperature than the rest of the system. During the compaction/deformation processes this grain boundary phase melts and assists in mass transport for grain growth or densification, which is a well-known effect generally occurring during hot deformation of Nd-Fe-B magnets.

P22/line 10: this cannot be decided without correcting the curves with regard to thermal expansion and pressure effects.

Answer: Section has been deleted.

P23/line 44: If the thermal conductivity impacts the properties that much, does it mean that sample temperature significantly deviates from the measured temperature?

Answer: Exact temperature measurement of the sample especially during hot deformation is a challenging task. Usually, temperature is measured by pyrometer at the bottom of a hole drilledI in one of the punches. Since there is a distance of several mm between the measurement point and the sample, deviations between sample temperature and measured temperature are possible. This effect might become more pronounced during hot deformation in a FAST/SPS device, since the semi-finished part does not have a contact to the die walls at the beginning of the deformation.

P30/line 8: Why are HP and SPS complementary? The anisotropy comes from the hot deformation step.

Answer: Terminology in this work has not been so clear up till now. SPT is the name for the hot deformation step in this work and is where anisotropy is induced. FAST/SPS is the stage where the compact is pre-sintered/hot compacted (similar to hot pressing). Anisotropy should not develop at this stage.

P33/line 36: new results should not be introduced in the conclusion. (also in the next paragraph)

Answer: Noted, conclusion does not introduce new results anymore.

The authors initially claim electroplasticity to be an important mechanism for densification. In the end of the results section, it is stated that this only happens in flash sintering, what makes sense. Still, without any local temperature control, identifying electroplasticity for increased densification without any further discussion is quite farfetched.

Answer: We agree that we only speculated on the occurrence of electroplasiticity without having any experimental confirmation. Therefore, we omitted the discussion of electroplasticity in the revised manuscript completely.

Overall, the paper is excessively long, describing in detail and repetitively what was done and what was not done, without being structured. The different sections are consequently mixed up. As this is not a Ph.D. thesis, the article can only benefit from being 1/3 to ½ shorter. The quality of the figures is good.

Answer: We completely restructured the paper only focusing on spark plasma texturing Nd-Fe-B magnets starting from semi-dense and dense compacts now. The part on Flash SPS was omitted. Therefore, the length of the manuscript was decreased by around 1/3, which hopefully improves the clarity of the presented results.