## Slide 1: PM by SPS
Sample list

## Slide 2: Pure MQU F samples
Sample | HC | HD | notes | 
1 | 241 | - | Ref sample | 
2 | 242 | 255 | 50MPa | 
3 | 243 | 256 | 60 MPa | 
4 | 245 | 260 | 70 MPa, Temp contorl issue | 
5 | 246 | 261 | 70 MPa, Temp contorl issue | 
6 | 247 | 266 | Best sample, 70 MPa, 75°C/min | 
7 | 248 | 268 | 70 MPa, temp ramp 50°C/min | 
8 | 249 | 269 | 70 MPa, temp ramp 75°C/min | 
9 | 250 | 270 | 70 MPa, temp ramp 100°C/min | 
10 | 251 | 266 | Test for 80 MPa, HC sample was cracked | 
11 | 252 | 271 | Test for 80 MPa | 
12 | 253 | 272 | Test for 80 MPa | 
13 | 254 | 273 | Test for 80 MPa | 
All results are in the presentation HC_and_HD_magnets_by_SPS_1.pptx Part I |  |  |  | 

## Slide 3: Mixed MQUF + 01072023 Samples
 | 0% Recycelt | 25% Recycelt | 50% Recycelt | 75% Recycelt | 100% Recycelt
1 | HC279 OH/HD293 OK | HC289 OK/HD294 OK | HC286 OK/HD295 OK | HC283 OK/HD296 OK | HC277 OH/HD297 OK
2 | HC280 OK/ ref sample | HC290 OK / ref | HC287 OK/ ref | HC284 OK/ ref | HC278 OH/ ref
3 | HC281 OK HD299 OK | HC291 OK / HD320 OK | HC288 OK/ HD318 F | HC285 OK/HD136 OK | HC292 OK/ HD298 F
4 | -- / -- | HC302 OK/ HD311 F | HC305 OK/ HD319 OK | HC309 OK/ | HC307 OK/ HD313 OK
5 | -- / -- | HC303 OK/ HD312 OK | HC304 OK/ | HC310 OK/ | HC307 OK/ HD315 OK
All results are in the presentation „HC_and_HD_magnets_by_SPS_2.pptx” and “HC_and_HD_magnets_by_SPS_3.pptx” (Part II contains the result from the first series of HD Samples: S13, S25, S31, S41, S51 and S54) (Part III contains the result from the second series of HD Samples: S13, S23, S34, S43, S55) |  |  |  |  | 

## Slide 4: Pure 01082023 Samples
Sample | HC | HD | notes | 
1 | 321 | - | Sample killed | 
2 | 322 | no | Ref sample for HC @ 750°C | 
3 | 323 | 327 | HD @ 825°C, HCS not full dense! | 
4 | 236 | no | Ref sample for HC @ 825°C | 
5 | 328 | 329 | HD @ 825°C, HCS OH | 
6 | 330 | 334 | HD @ 825°C | 
7 | 332 | 335 | HD @ 775°C | 
8 | 333 | 336 | HD @ 800°C, Best sample | 
All results are in the presentation HC_and_HD_magnets_by_SPS_4.pptx Part IV |  |  |  |