Review

The manuscript is well written and presents an interesting result, however needs some improvement and it would be nice if the authors could provide some additional information about the exact motivation for the choice of some experimental parameters (reference to literature or theoretical calculation) e.g:

- Why was the weight ratio of 4:1 La0.7Ce0.3Fe11.6Si1.4 to Fe powders chosen?

- How the layer thickness 0.2 mm for the Fe and 1mm for the LCFS layers was chosen?

On p.4 l. 51 the authors write about “microcracks generated during hydrogenation.” Would be nice to include a micrograph of hydrogenated sample to the manuscript.

On Fig.2 (d) the anisotropy of the thermal conductivity is indicated to be an axial and not, as has to be expected, as a planer effect.

The thermomagnetic curves presented on Fig 3 (a) are measured in magnetic field of 0.05 T, so it is more precise to represent them as normalized magnetization.

On p. 7 l. 10 the authors wrote: “Under the 1 T field change, the average maximum ΔT value of LCFSH/Fe composites is determined to be 2.1 K at 315.5 K, suggesting that a high performance permanent magnet can effectively induce phase transition as a magnetic field source.“ Could the authors explain this better? A look at the magnetization isotherms shown in Fig. 3 (b) shows that the phase transition is induced up to 316 K at a very low magnetic field and is almost complete at 1 T, which is why a permanent magnet can be used as a magnetic field source. Is this correct?

It may be beneficial for readers to divide Fig. 4 into two parts, as the ΔT curves in Fig. 4(a, b) are not directly connected to the rest.

Fig. 4 (c) and (d) represent the main result of this work and require a more detailed but easy-to-read presentation.  The authors can probably enlarge Fig. 4 (c) and place the corresponding IR images on the T vs. t curve.

On p. 3 l.13 the experimental set-up is described as follows “sample holder was equipped with a circulating water heater”, while in Fig. 4 (d) it looks as if the temperature of the sample holder was constantly increasing during the 200 seconds in which a magnetic field of 1 T was applied. Is this a real effect?