Our ultimate goal is to establish a reliable recipe for production full dense hot deformed magnets by SPS. We need understanding of the processes at each step, so we can in future easily adjust the main processing parameters (time, pressure, temperature) according to the specific powder characteristics (grain size, crystallinity, composition etc.).

To fulfil this, we have to do systematic sample characterisation on each step

A. Powder

- Properties of the scrap magnets (for recycled powder only)

  - Chemical composition

  - Contamination / Oxidation

  - Magnetic properties

- Induction molten ingot

  - Chemical composition

  - Contamination / Oxidation

- Melt spun ribbons (to be repeated in case additional heat treatment is performed)

2.1 Microstructure

2.2 Contamination / Oxidation

- Ball milled melt spun ribbons

3.1 Chemical composition

  - Contamination / Oxidation

  - Magnetic properties

B. Hot compaction

- Use DSC to define the THC (displacement test if not available)

- Produce HC samples at THC-25 THC and THC+25

  - Check sample density

  - Adjust pressure to obtain full dens HC samples

- Sample Characterisation

  - Chemical composition

  - Contamination / Oxidation

  - Magnetic properties

  - Based on the results from 3 choose the right

Magnetic properties

C: Hot deformation

1.1 Pre